### PRE-POUR QUESTIONS

#### General

#### 1. Has a mix design been completed & approved by the engineer?

# 2. Has the concrete plant been checked by WisDOT?

# 3. Have the scales been checked and certified?

4. What time will pour begin?

# 5. Where will the pour begin?  If bridge deck, which end will the pour begin?

6. Rate of concrete delivery?

| Delivery (501.8.2) | < 60 F w/o retarder | 60 F w/o retarder | 60 F w/ retarder * |
| --- | --- | --- | --- |
| Agitating Truck | 1.5 hours | 1 hour | 1.5 hours |
| Non-Agitating Truck | 30 min. | 30 min. | 30 min. |

* If using fly ash or slag with retarder or doubling dosage of water reducer, dose on cement not total cementitious materials.

7. Any other pours from the same plant?

8. What is the truck route/trucking plan?  Number of trucks?  Discuss truck delivery on construction site so that this route can be cleared and there is enough room for maneuvers.

If necessary, have all interested parties (residents, emergency responders, road maintenance sections, etc.) been notified?

Discuss traffic control requirements.

9. Number of men on pour?

Vibrators should be used properly.  It will not be used to move material around.  Insertion is vertically.

10. Number of finishers?  Determine if that is enough finishers to complete work satisfactorily.  Blessing the concrete will not be allowed.  The use of sprayers that deliver a fine mist with an approved rewetting product is the only acceptable method for finishing.

#### 11. Is the loader operator familiar with loading plant, working stockpiles, and does loader operator know which stockpiles are for this project?  Have the operator review the procedures.

12. Will concrete be poured underwater? If so, review section 502.3.5.3.

13. All areas formed for concrete shall be free of debris prior to pour – paper, wood, saw dust, etc.  The deck shall be hosed clean if necessary.

14. Steel reinforcing shall be clean of debris prior to pour – tape, mud from walking on steel, etc.

15. Has the steel been tied properly and is it stable under foot?

16. How will water for dampening the forms/cooling steel be delivered?

17. What is the contractor’s method of placement? (bucket, pumper, conveyor, slip form, forms, etc)

For Bridge – Abutment, Pier, Deck

For Paving/other – Mainline, Intersections, Curb & Gutter, etc

18. What is the required finish on the deck?

19. When a pump is used, the sample is obtained from discharge of the pump. Air losses across a pump will not exceed 1.0 %.

20. Material shall be delivered as close a possible to its final position.  Using a vibrator to move material around will not be allowed.

21. What will be the procedure if a load fails air or slump test?  Will drying load, adding air on site, more revolutions, etc. be allowed if load fails?  If so, is an area available for the truck to charge?

22. Ready mix trucks equipped with an operating revolution counter?

23. Is there a back up plan if there is a breakdown?

24. What is the plan for emergency joint placement?

# 25. What will be contractor’s method of curing?

Bridge – wetted burlap, approved product, polyethylene sheeting – if a curing compound will be used make sure it is on the approved list.

Paving or incidental - Approved curing compound? (check date and containers, if older than 1 year, must be re-tested)

#### 26. What provisions are being taken for inclement weather in the middle of the pour?

27. For structures, how will supplier control temperature of the mix? (< 80 degrees)

28. Is cold weather expected?  If so, have all provisions under Section 501.12 been followed?

# QMP Projects - General

29. Is a QC plan required?  If so, has the QC plan been submitted and approved?

30. Mix design changes must be approved prior to use.  Any mix design or placement method change requires a new lot. See Standard Specifications section 715.3 for lot specifications.

31. Names of those responsible for testing?

- QV (State)

- QC (Contractor)

- IAP

32. Are these individuals at the meeting?  Sampling and testing logistics are discussed at the pre-pour meeting, so the actual technician performing those duties should be present.

33. How will the test results be disseminated to those responsible – especially the engineer?

34. Who is responsible for rejecting loads if QC tests fail?  Is that individual prepared to reject loads?

35. The QC tester will remain on site until end of each pour.  Engineer can order more testing if desired.

36. Where will testing occur?  Is it level? (location for slump, air, cylinders, gradations)

37.  If a night pour, lights should in the materials testing area.

38. Is a wheel barrel available for State use?

39. Where should tested materials be deposited?

40. Tests to be performed by QC during concrete production and placement.

## a)	If no production records, aggregate gradation testing must be completed during concrete production.

Have the production records been submitted to the engineer?

Do production records conform to gradations in QC plan/mix design?

b)	Aggregate moisture content (w/c ratio is calculated and recorded)

c)	Materials finer than 75 microns (P200)

d)	Compressive strength cylinders

e)	Air content

f)	Slump

g)	Concrete temperature

41. How many technicians will be available to test during placement?

For the proposed delivery rate, is that enough technicians to adequately test material so that testing is completed satisfactorily and placement is not slowed?

# 42. Where are cylinders to be stored and/or delivered?

43. Where will cylinders be placed for initial curing, prior to taking to lab?  There will be 3 cylinders per sublot for paving and structures and 2 cylinders per sublot for ancillary, is there enough room?  Curing temperature must be between 60 and 80 degrees. A minimum/maximum thermometer should be used.

QC & companion cylinders – for up to 48 hours

44. Where will engineer’s cylinders be placed for initial curing?