## Slide 1: Project Leadership Workshop Materials - 2018
March 13, Rhinelander

## Slide 2: Staffing
Rhinelander
John Brophy
715-493-3085
Lab
715-365-5735
Wisconsin Rapids
Jeff Michalski
715-421-8339
715-459-4791
Lab
715-421-8060

## Slide 3: HMA
Project staff responsibilities.
Selecting all QV random numbers.
Collecting all QV samples.
Collecting all QC retained samples.

## Slide 4: Collecting QV samples
Correct
Incomplete

## Slide 5: A change in HMA mix designs
A change in AC grade.
Same mix design, same 250 number.
Example:
4 LT 58-28S
4 LT 58-34S
Changing from a HMA (275 degrees) to a WMA (235 degrees) design.
Is a different mix design, needs a different 250 number, and another set of random numbers.

## Slide 6: Ignition oven
Will be run on all HMA samples for PWL projects to check AC content.
AC content will be run on regular QMP projects starting in 2019.
Aggregate correction factor specific for each oven and mix design.

## Slide 7: HMA – Air Void Regression
ASP-6, December 2016 lets.
Mix designs, still design to 4.0% air voids in lab.
Lowered to 3.0% air voids (target) in the field.

## Slide 8: HMA – Dispute Resolution
QV sample falls outside of 2.0 – 4.3% air void range.
C.O. Materials will test the QV retained (that failed) and any needed forward and backward QC-retained samples (until they pass).

## Slide 9: 2018 PWL projects
1166-12-80, I-39, Plainfield to Stevens Point, Portage County
  4 LT 58-28S 7970 tons
  4 MT 58-28S 49500 tons
  4 MT 58-28H 1500 tons
1600-22-81, Clintonville, Shawano County
  3 MT 58-28S 22380 tons
  4 MT 58-28S 17407 tons

## Slide 10: 2018 PWL projects
6380-04-77, STH 97, Stratford to Goodrich, Marathon County
  5 LT 58-28S 35560 tons

## Slide 11: 2018 PWL projects
Start up day requires 5 day notice (by specification).
Pre-pave meeting with contractor.
Pre-pave meeting between project staff and regional materials.

## Slide 12: WisDOT Longitudinal Joint
Special Provision
Plans are to add this to a couple of 2018 construction projects.
$0.40 / linear foot pay adjustment.

## Slide 13: WisDOT Longitudinal Joint
(6) Minimum reduced by 1.5% at longitudinal joint with lateral confinement.
(7) Minimum reduced by 3.0% at longitudinal joint with no lateral confinement.

## Slide 14: AC sampling frequency (new)
Truck sample – optional on all project.
In-line sampling based on one per 15000 HMA.
Projects under 1000 tons of mix in-line sample is optional.

## Slide 15: AC sampling frequency
All AC samples must be observed by a DOT representative (no exceptions).
Include full name on sample card.

## Slide 16: Tack coat
One sample per project for quantities greater than 2500 gallons.

## Slide 17: Base course – stockpile sampling
Stockpile sampling prior to placement for each grade and each source.
QV (X > 500 tons)
QC (no minimum)
QV and QC are separate samples, but done at the same time.

## Slide 18: Base course – random numbers
Materials audit issue - QV random numbers.
Audit emphasizes the need to compute, document, and retain in your materials records.
Jeff and I will check as part of our materials field reviews.

## Slide 19: QV base course – stockpile and placement
Must notify the contractor’s Materials coordinator by email two hours before sampling to allow for contractor to witness the sampling.
Results need to be back to the contractor in two business days.

## Slide 20: Dropping off of samples
Security codes, available on request.
QMP samples – two day turnaround.
Central Office samples – Stores truck (two week cycle).

## Slide 21: Sample sizes
Sample sizes, keep to 60 pounds maximum.
Buckets.
Bags, moisture is critical.

## Slide 22: Importance of observing sampling
Asphalt cement.
Hot mix asphalt samples.

## Slide 23: IA reviews
IA goal is review all samplers and testers on our projects.
John Brophy 715-493-3085
Jeff Michalski 715-459-4791

## Slide 24: Questions and Answers