Coordinate with Soils Engineer and discuss the highlighted option before including in special provisions.

1. Select Borrow

*Add the following to standard spec 208.2.1(2):*

Furnish and use material that consists of granular material meeting the following requirements: Not more than 25% of that portion passing the No. 4 sieve shall pass the No. 200 sieve.

If the engineer approves, the contractor may substitute Breaker Run conforming to standard spec 311 for select borrow.

ner-208-010 (20190717)