This is NOT the preferred mix. Use TRAFFIC BOND LIMESTONE 3/8-INCH special provision unless trail owner (County, DNR, etc) requests this mix gradation.

1. Limestone Screenings 3/8-Inch, Item SPV.0195.##

A Description

This special provision describes providing 3/8-inch limestone screenings. Conform to standard spec 301 and 730 and as follows.

B Materials

Provide limestone screenings conforming to the following gradation requirements:

|  |  |
| --- | --- |
| Sieve Size | % by Weight Passing |
| 1/2-inch | 100 |
| 3/8-inch | 65-92 |
| No. 4 | 45-75 |
| No. 8 | 30-55 |
| No. 30 | 15-35 |
| No. 50 | 10-25 |
| No. 200 | 5-10 |

Provide QMP for limestone screenings according to standard spec 730.

C Construction

Construct the limestone screenings conforming to standard spec 301.3.

Compact a maximum of 6-inches for each layer at a time.

D Measurement

The department will measure Limestone Screenings 3/8-Inch by the ton acceptably completed.

Conform to 301.4(1).

E Payment

The department will pay for measured quantities at the contract unit price under the following bid item:

ITEM NUMBER DESCRIPTION UNIT

SPV.0195.## Limestone Screenings 3/8-Inch Ton

Payment is full compensation for preparing the foundation; and for furnishing, stockpiling, placing, shaping, compacting, and maintaining the limestone surface throughout construction.

Ner-301-005 (20190710)