Used this preferred mix gradation for recreational trails unless the trail owner (County, DNR, etc) requests a specific gradation.

1. Traffic Bond Limestone 3/8-Inch, SPV.0195.##

A Description

This special provision describes providing 3/8-inch traffic bond limestone. Conform to standard spec 301 and 730 and as follows:

B Materials

Provide limestone conforming to the following gradation requirements:

|  |  |
| --- | --- |
| SIEVESIZE | PERCENT PASSING BY WEIGHT |
| 3/8 inch | 100 |
| No. 4 | 80 – 95 |
| No. 40 | 65 – 86 |
| No. 100 | 25 – 40 |
| No. 200 | 8 - 25 |

Provide QMP for limestone according to standard spec 730.

C Construction

Construct traffic bond limestone conforming to standard spec 301.3.

Two days after the limestone screenings have been placed or when the screenings are dry and firm, taper the edges of the limestone screenings using the drivers' side wheels of a truck. Compact and roll the edge of the limestone screenings to create a neat bevel.

D Measurement

The department will measure Traffic Bond Limestone 3/8-Inch by the ton acceptably completed.

Conform to 301.4(1).

E Payment

The department will pay for the measured quantity at the contract unit price under the following bid item:

ITEM NUMBER DESCRIPTION UNIT

SPV.0195.## Traffic Bond Limestone 3/8-Inch TON

Payment is full compensation for preparing the foundation; and for furnishing, stockpiling, placing, shaping, compacting, and maintaining the limestone surface throughout construction.

ner-301-015 (20190710)